Products:

2. Lined Fittings

4. Lined Lateral Tee

VescoaT supplies and manufacturer of PTFE Lined Lateral Tee, We also manufacture in PFA / FEP / HDPE lined Lateral Tee by using most advance and hitech techniques. Non Standard size available on request.

| Dimension Detail: |  |  | All Dimensions are in mm |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| NB |  | d4 | K | D | B1 | No. of Holes & Hole Dia |
| MM | INCH |  |  |  |  |  |
| 25 | 1" | 50.8 | 79.2 | 108 | 14.5 | 4 x 15.9 |
| 40 | 1.5" | 73.2 | 98.6 | 127 | 17.5 | 4 x 15.9 |
| 50 | 2" | 91.9 | 120.7 | 152.4 | 19.5 | 4 x 19.0 |
| 65 | 2.5" | 104.6 | 139.7 | 177.8 | 22.2 | 4 x 19.0 |
| 80 | 3" | 127.0 | 152.4 | 190.5 | 24.0 | 4 x 19.0 |
| 100 | 4" | 157.2 | 190.5 | 228.6 | 24.0 | 8 x 19.0 |
| 150 | 6" | 215.9 | 241.3 | 279.5 | 25.5 | 8 x 22.2 |
| 200 | 8" | 269.7 | 298.5 | 342.9 | 29.0 | 8 x 22.2 |
| 250 | 10" | 323.9 | 362.0 | 406.4 | 30.5 | 12 x 25.4 |
| 300 | 12" | 381.0 | 431.8 | 482.6 | 32.0 | 12 x 25.4 |

Technical Specification:

| Size | 20NB TO 300NB ( ¾” TO 12” ) |
| --- | --- |
| Length | As per Standard of B16.5 & ANSI B 16.42 |
| Liner | PFA - Per Fluoro Alkoxy, ASTM D3307 FEP - Fluorinated Ethylene Propylene, ASTM D2116 HDPE - As per Standard |
| Body | As per ASTM A 234 Gr. WPB / DI A395 / SS304 / SS316 ( Seamless) |
| Steel Housing | Carbon steel or Stainless Steel |
| Flanges | ASTM A 105 (N) / IS 2062 / ASTM A351 GR CF8 & CF8M |
| Drilling / Pressure | ASA 150# / 300# / DIN / Table – F |
| Dimensional STD | Lateral Tee : B16.5 & ANSI B 16.42 Flanges : ASME B 16.5 Lining Standard : ASTM F 1545 |
| Temperature | -29℃~200℃ |
| Vacuum | Full vacuum rated |

| Testing/Inspection |  | Mechanical Properties |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  |  | PTFE | PFA | FEP |
| Hydro Test | At 29 Bar, after lining | Tensile Strength, PSI (min) | 3500 | 3800 | 3000 |
| Spark Test | At 25 KV | Elongation, % (min) | 300 | 300 | 250 |

Notes :

1. All Lined Lateral Tee have Fix Flange on Both Side ( SOFF flange both side with one end loose flange and fixed flange at the other side or Both Side Loose Flange as on Request) For A105 Flange:  lap joint flange at one end and fixed flange at the other end.

2. Suitable vent holes are provided for all fittings.

3. All Fittings work will be supplied with suitable wooden end covers to protect the flare faces.

4. Material test certificates will be provided for all raw materials

5. The plastic liner flare will replace the raised face portion of the flange.